## Slide 1
Possible that the oleic acid is not uniform, e.g. has its own core-shell structure:
NaCl
oleic acid, behavior 1
oleic acid, behavior 2
Possible that the NaCl core does not contribute much to scattering, I’m not sure
Known core: NaCl, diameter ~50 nm
Known shell: oleic acid (C18H34O2), outer diameter ~1 um
NEXAFS of oleic acid across the carbon K edge shows a clear C-C double-bond peak and step in signal, as expected. (Disregard the “with ozone” data for now.)
I don’t have a measurement for NaCl but its properties should be fairly constant in this range
I can’t guarantee spherical symmetry but it seems likely enough to try models that assume it

## Slide 2
My first pass at fitting: treated particles as uniform (non-interacting) spheres
  Modeled my signal as a sum of signal from 3 size distributions (of spheres), adding up to the overall size distribution shown in red
    Most of the obvious shape comes from the component with a diameter near 1 um (black line in inset plot; dashed line on main plot)
    Trying to model the NaCl core didn’t make an obvious difference

## Slide 3
My first pass at fitting: treated particles as uniform (non-interacting) spheres
  Curves at different energies have clearly different size-related features
    With naïve modeling (not adjusting for different optical constants at different energies), particles look larger when in resonance with the C edge
      My fits gave a difference in diameter of nearly 100 nm, which doesn’t make physical sense
      Cheng said this behavior makes sense for a core-shell structure with contrast between layers changing as energy changes

## Slide 4
I don’t have tools that let me consider the changing optical properties near the carbon K-edge in a way I trust
  I know that it’s possible to estimate optical constants from the NEXAFS (I think I sent you a csv) and I’m hoping that information will be enough to come up with a plausible model
  If I were doing the modeling, I’d start with the known NaCl core and the rest of the particle as uniform oleic acid, and if that didn’t work see if it was possible to come up with a core-shell structure (with a larger core, or similar) that did make the model make sense
    I realize that’s quite open-ended, and understand if you don’t have time to do the second part

## Slide 5
Fitting parameters

## Slide 11
278.9 eV